L10 - 	WINDOWS

316	STEEL WINDOWS AND DOORS:

-	Manufacturer and reference: Crittall Windows Ltd, Corporate™ W20 range

-	Generally manufactured in accordance with BS 6510, W20 section.

-	Weathertightness:  To BS 6375: Part 1

Exposure category (Design wind pressure):  1200/2000 (Pa) see Table AA

-	For air permeability, water-tightness and wind resistance data see Table AA

-	Operation and strength characteristics:  To BS 6375: Part 2

-	Construction:  All frames have welded corners and are flat and square within normal	manufacturing dimensional tolerances of +/- 1.5 mm.  Intermediate bars are hot tenon riveted.

-	Galvanising:  All components including steel attachments, coupling members and ancillaries:  hot-dipped after manufacture to BS EN ISO 1461:1999

-	Glazing details:  Will accept double glazing up to 16 mm in thickness.

Glazing beads present no horizontal ledges on which dust and dirt can gather.

-    	Weatherstripping:  Gaskets complying with BS 4255: Part 1 manufactured from EPDM	secured into grooves of opening frame with adhesive.

-	Ironmongery/accessories:  See clause 328.

-	Finish as delivered:  Galvanised or Duralife™ (see clause 331) in a range of colours.

325	STEEL WINDOWS AND DOORS:

-	Generally all the foregoing.

-	Manufacturing undertaken in the Crittall factory by directly employed personnel.

-	Design testing, manufacture and installation carried out under Quality Management Systems certified to BS EN ISO.9001

328	IRONMONGERY/ACCESSORIES:

-	Standard provisions:  See Brochure/Binder

-	Standard finishes:  Satin anodised or satin chrome according to fitting.

-	Optional hardware/finishes:  Available, consult Crittall.

331	FINISH COATING

-	Type/reference:  Epoxy free Duralife™ polyester powder coating using Interpon D36 powder.

-	To BS 6497

-	Preparation:  Following galvanising, windows are chemically cleaned and pre-treated to provide surface to which powder coating will adhere.

-	Covering:  Minimum 60 microns on all significant surfaces.

-	Colours:  Wide selection available.  See Crittall Colour Selector.

-	Process:  Coating will be undertaken in the same manufacturing plant as the frame fabrication.

552	METAL GLAZED SCREENS:

-	Screen/composite window assemblies are available utilising all Crittall ranges.

-	A full design/advice service is available.

-	Coupling details; consult Crittall.

## Table AA

| TYPE OF OPENING LIGHT | EXPOSURE CATEGORY (Pa) | AIR PERMEABILITY: Not More Than 16m3/h/m JOINT, AT (Pa) | WATER TIGHTNESS: NO LEAKAGE, AT (Pa) | WIND RESISTANCE: NO DAMAGE & ONLY PERMISSABLE DEFLECTION, AT (Pa) |
| --- | --- | --- | --- | --- |
| Corporate™ W20 |  |  |  |  |
| Vertical Pivot | 1200 | 300 | 50 | *1200 |
| Horizontal Pivot | 1200 | 300 | 100 | *1200 |
| Bottom Hung Open In | 1200 | 300 | 100 | *1200 |
| Side Hung Open In | 1200 | 300 | 100 | *1200 |
| Side Hung Open Out | 2000 | 300 | 300 | 2000 |
| Top Hung Open Out | 2000 | 300 | 300 | 2000 |

* A higher wind resistance can be achieved.